## Slide 1: Using MINOS scintillators as a surface veto
Delia Tosi / Chris Wendt
UW Madison

## Slide 2: References for these slides
Slides from MINOS workshops, for example:
  http://www-off-axis.fnal.gov/workshops/stanford03/transparencies/michael_minosscin.ppt
Public reports, for example:
  www-numi.fnal.gov/minwork/info/tdr/mintdr_5.pdf

## Slide 3: Basic unit
1.0 cm x 4.1 cm Dow Styron 663 W polystyrene + wavelength shifters PPO (1%) and POPOP (0.03%) [ 300 T, 600 km of 4.1 cm2]
WLS Fiber: Kuraray double-clad 1.2 mm diam., 175 ppm Y11 : shifts blue light to green [780 km]
8 m
TiO2 CAP Reflector
Clear groove
Notes:   WLS fiber1.20 +0.024 -0.005 mm diam.
  175 ppm Y11 fluor (K27)
  polystyrene core, double clad (PMMA and polyfluor)
“Non-S Type” PS core is of almost no oriented polystyrene chain and is optically isotropic and very transparent.
This conventional standard type has good attenuation length, but it showed weakness against cracking caused by bending or handling during assembling.

## Slide 4: Test performed on strip and unglued fiber
Strip and fiber were put in freezer and temperature was cycled a few times down to -80 C (in steps and in one shot)
Stress test (banging the strip against solid surface) was performed several times imposing harsh temperature change
TiO2 does not show any sign of deterioration, fiber looks good and kept flexibility

## Slide 5: Module tests
We got 4 pieces of scintillator panels from MINOS far detector:
  2 pieces have optical connectors (OC)
  2 pieces have no connectors
Cables:
  2 (clear fibers): OC assembly  OC assembly
  1 (clear fibers) : OC assembly  single fibers
Electronics:
  MCPMT assembly + 2 “cookies” to feed fibers (see slides later)

## Slide 6: Far detector module layout
8 modules per plane
Four 20-wide modules in middle
Four 28-wide modules on edges
Two center modules have coil-hole cutout
Coil Bypass
28
28
28
28
20
20
20
20
90’’ ~ 2.3 m
  Clear Fiber: Like WLS, no fluor, 1100 km of fiber built into cables with 20/28 fibers.

## Slide 7: Module overview
Module: assembly of scintillator strips wrapped by aluminum sheets.
WLS fibers are routed through end manifolds to bulk optical connectors.
Modules, connectors and cables are light-tight (until you open them).
Assembly Drawing for manifold
Bottom Al Cover
Bottom Al light case
Top Al light case
Top Al cover
Fiber routing
manifold
Connector
Top variable
width seal
Bottom variable
width seal
Light injection
manifold
Light Case
Manifold base with fiber grooves
Formed Al cover
Light injection cover
Variable width seal
Optical
connector
Module parts for “straight-out” manifold

## Slide 8: Cables

## Slide 9: Electronics
Spring loaded PMT base
M16 PMT
PMT jacket
Adjustable mounting
bracket (alignment)
Alignment
window (not
installed)
Cookie with fibers
PMT Mounting
Components
Fiber Layout
Hamamatsu R5900 multi-anode PMTs:
  16 pixel tubes for the far detector (pixel size 4mm x 4mm)
  64 pixel tubes for the near detector (pixel size 2mm x 2mm)
Gain of 106 consistent to x2 (M16) or x3(M64)
QE at 520 nm typically 13.5%
Good single pe peak
Very fast signals and low time jitter.
Notes: The 384 signal fibers are routed to three Hamamatsu M multichannel PMTs through precision machined cookies. Eight fibers are routed to each 4mmx4 mm pixel. Two of the PMTs in a far detector MUX box see 8 x16=128 fibers from single planes the third PMT sees 8x8=64 fibers from each plane The ribbon cable connectors are inserted into the front plate according to a pattern that minimizes fiber lengths within the MUX box

## Slide 10: Expected performance
Number of observed photoelectrons
Distance along the module (m)
Individual Strip Responses
From reference
Light output: 10.6 p.e. reading out from both sides for a 2 GeV muon (5.5 p.e. min)
Time measurement: < 2 ns per strip for signals > 10 p.e.
Calibration:
  Relative near/far energy response to within 2%
  Absolute hadronic energy response to within 5%.
Performance variation vs time:
  Decay of fluors
  Monitored with calibration devices (laser, muons)
Do we need to include a calibration device in out prototype?

## Slide 11: Making our own small test module
W = 32 inches
L = 24 inches
Fits in the Chamberlin freezer

## Slide 13
Toray PFDU-FB1000

## Slide 14
Fiber connected to 2” PMT Hamamatsu RD2759 (2kV – 1e7 gain) connected to mainboard
DOM Platypus placed under strip and connected in LC mode
Notes: Optical fiber is Toray PFDU-FB1000 (datasheet is in our elog at http://elog.icecube.wisc.edu/AbsCal/154 )
It's 1mm diameter, most of that is PMMA core and then there is the thin fluoropolymer cladding for internal reflection, see the datasheet if you want more detail. There is a graph in there showing no effect of operating at -55C, by the way.
The DOM is called "Platypus", it was one of two that were used by John Kelley & Jim Braun for testing when developing the DOMCal program. The other one in there is "Titanium".
The 2" PMT is Hamamatsu H7195, serial number RD2759 (the same one as mentioned in the elog entry above). We run it around 1e7 gain.

## Slide 15: Test of mini module
Goal of planned test:
  How much light we get from a muon?
  Glue is expected to brittle at low temperature. Does this effect the light output? By how much?
  Planned test:
    Run at room temperature and verify we can see a signal
    Monitor performance vs decreasing temperature
    Inspect visually the assembly after temperature cycle
We ran a first test at room temperature
Computer died shortly afterwards so we have not gone down in temperature

## Slide 16: Platypus DOM plots
Ch1 muon signal at 360 mV ~ 65 SPE
1 SPE signal in Ch0 at ~6 mV
We select pulses in sync -100 ns to +100 ns to a signal in ch1 DOM > 0.2 V

## Slide 17: Scintillator plots
Peak at 2.5/1.2=2 SPE

## Slide 18: What’s next
Set up a new computer to take data
Take measurements at room and low temperature
  Possibility to improve coupling with splice and coupling gel
  Need a plan B if glue fails catastrophically
Switch to electronics for deployment
Test the whole setup in freezer at PSL

## Slide 19: If we need to build something different
Many things can be studied and improved:
Light output dependencies:
  Light output <linear with scintillator thickness but depends on aspect ratio.
  Light output inversely proportional to strip width (actually about 1.3x for 2 vs 4 cm.)
  Light output with two fibers = 1.8x light with one fiber.
  Light output vs fiber radius ~ R1.3
Difference between fiber in hole vs fiber in groove:
  A fiber glued into the groove is 1.8 times better than a dry fiber
  A dry fiber in the groove is 10% worse than a dry fiber in a hole
Increase thickness? or use more strips on top of each other?

## Slide 20
Backup

## Slide 21
The most significant design critereon for the far detector was the light output.
  >4.7 pe’s/muon (2 GeV muons) for the average sum of two strip ends.
The measured light output is almost a factor of two higher than the design requirement.
Light output measured for all strips for muons in the far detector. The light output is corrected to 1 cm pathlength per plane but is not corrected for PMT gain variations.
Mean = 10.6 pe’s
(~8.5 for 2 GeV muons)
Average light output for one-side of readout vs plane number in the detector. (Not corrected for pathlength or gain variations). This shows the uniformity in the hardware and raw response.
Light output at the far detector
Light output is stable!
From reference

## Slide 22
The time resolution of the MINOS scintillator system is determined primarily by the decay time of the Y11 fluor in the WLS fiber ~ 8 ns.
The time resolution for each scintillator strip is expected to be ~2.5 ns based on the photoelectron statistics for muons.
Current measurement of resolution using downgoing muons in the far detector is s=2.6 ns/plane.
The direction of muons can be determined with ~ 10 planes for contained vertex events.
To distinguish upgoing from downgoing through-going muons ~ 20 planes are needed.
Time Resolution in the Far Detector
Distribution of measured time residuals for muons
Passing through all strips in the far detector. The
Time resolution of 2.6 ns is calculated from this data.
From reference

## Slide 23
Connector pair
Spring loaded PMT base
M16 PMT
PMT jacket
Adjustable mounting
bracket (alignment)
Alignment
window (not
installed)
Cookie with fibers
PMT Mounting
Components
Front-end
electronics
Far detector (shown)
  3 M16 PMTs/box
  8 fibers per pixel
PMT Boxes and Connectors
View of PMT
boxes installed
on the far detector

## Slide 24
    EDIA/Setup Production Total
    $k $k $k
Scintillator System 2950 12100 15050
  Scintillator 750 2430 3180
  WLS Fiber 220 1170 1390
  Module Components 400 1400 1800
  Module Fabrication 1100 2400 3500
  Clear Fiber Cables 100 2090 2190
  PMTs 180 1670 1850
  PMT Boxes 200 940 1140
Readout Electronics (32k channels) 4500
Steel 1000 3500 4500
Installation 1000 3800 4800
Cavern/outfitting 12000
Scintillator system cost/m2 $470 $580
Scale-up by factor of ~4? $330 $400
Overview of Costs (Far Detector Only)

## Slide 25
Scintillator Module Components
  Extruded Scintillator
    MINOS Cost = $9/kg (about 2 m) includes QC checks, handling, delivery.
    New die ~$10k
    New profile ~$50-100k (depends on how radical the changes are)
    New vendor ~$100k+ (depends on competence of vendor)
    Kuraray: MINOS quote ~$13/kg… MINOS did not accept. This was the only competing offer.
  WLS Fiber:
    MINOS cost = $1.55/m
    On average need Lscin + 0.7m x (1,2)
    Small production cost ~ $3.50/m (~10km)
    Cost scales as ~R2 and light as R1.3. Biggest practical radius was good value for MINOS but maybe not if lower light is OK. MINOS fiber is 1.2 mm diameter. 1.4 mm is probably the largest possible using these techniques.
MINOS Building Blocks

## Slide 26
Scintillator Module Components (cont.)
  Aluminum ~ $12/m2 of module (2 skins)
  Manifolds, etc ~ $200/module (~$5-10k startup for different styles)
  Glues, expendables ~$12/m2 of module
  Connectors ~$5/ module
Scintillator Module Assembly
  ~20 hours/module for MINOS, style of module matters very little
  Setup for different style modules ~ 2 weeks = 800 hours
  Setup with MINOS equipment at new site and new crew ~ 4000 hours
  New equipment equivalent to MINOS ~ $400k.
  Cost at Caltech rate for MINOS ~$400/module
Full module costs:
  MINOS Cost: $660/module + $180/m2 : 8m module = $2100 = $260/m2
More MINOS Building Blocks

## Slide 27
Readout Component Costs
  Clear fiber cables
    $1.15/m for raw clear fiber
    $1.00/m for conduit
    $8/ cable for connectors and shrouds
    2 hours/cable assembly labor (~$44/cable)
    Example: 24 fibers x 4m = $170
  PMTs
    M16 ~ $760/tube + $40/base + $200/mounting +$400/routing box = $1400/tube
    In MINOS far detector: $1400/tube = $88/pixel = $11/fiber end readout (8fib/pix)
    M64 ~ $1300/tube + $50/base + $200/mounting + $400/routing box = $1950/tube
    In MINOS near detector: $1950/tube = $30/pixel = $30/fiber end readout (1fib/pix)
  Other stuff: (LEDs, HV…) ~$200k for a “small” system
  Electronics:
    MINOS far detector: ~$400k + $40/channel (pixel, $5/fiber end)
    MINOS near detector ~$600k + $200/channel (pixel/fiber end)
    DAQ system ~$300k
More MINOS Building Blocks